# Luxalon® 150F/200F Façade System

## Part 1. 150F/200F Façade System general

  - 1.1 Introduction

Supply and fix Luxalon® 150F/200F Façade System as manufactured by

Hunter Douglas Architectural Products.

  - 1.2 Description of the system

The system will consist of linear rollformed aluminium panels, which can

simply be slid into the prongs of a stringer. The stringers are fixed on a non-

Luxalon® sub-construction. To prevent contact corrosion by applying dissimilar

metals, each fixing of the stringers to the sub-construction must be made

through the Luxalon® washer set.

## Part 2. Product

________ m2 Luxalon® 150F/200F Façade System consisting of:

  - 2.1 Panels

150F: size 170 x 17 mm manufactured from 0.6 mm aluminium

200F: size 200 x 17 mm manufactured from 0.7 mm aluminium

Panels to be manufactured from pre-painted, stove enamelled aluminium,

corrosion resistant alloy EN-AW-3005 or equivalent (according to EN 1396 and

EN13523). Panels have a length of _________ mm (manufacturer availability

800-6000 mm, other lengths are available on request). Panels to be coupled in

longitudinal direction by means of panel splices or by means of the Luxalon®

horizontal joint extrusion.

  - 2.2 Stringers

Rows of 0.95 mm (150F) or 1.2 mm (200F) thick aluminium rollformed stringers

shall be installed at ________ mm centre to centre on a sub-construction

consisting of a supporting steel or aluminium framing of sufficient strength and

rigidity to provide resistance to wind-pressure/suction. Stringers are provided

with prongs to hold panels in a module of 150 mm (150F) or 200 mm (200F).

## Part 3. Additional specification

  - 3.1 Profiles

Edge, trims drip sections, capping etc. made of stove enamelled aluminium strip, with Luxacote® paint finish (± 30micron).

  - 3.2 Coating

Architect will make a colour selection from the standard Hunter Douglas colour range for Luxalon® exterior 150F/200F panels code no. ________ or a special colour will be made to match.

  - 3.3 Installation

All materials shall be installed in strict compliance with all local codes; ordinances and manufacturers recommendations including specific additional requirements as may be called for in the specifications or shown on the drawings.