LUXALON® WIDE PANEL 300L CARRIER SYSTEM SPECIFICATION


PART 1: CARRIER SYSTEM GENERAL

1.1 INTRODUCTION

Supply and fix Luxalon® 300L Wide Panel Carrier System as Manufactured by Hunter Douglas Architectural Products.


1.2 DESCRIPTION OF THE SYSTEM

The system will consist of panels fixed to an adjustable suspension system which allows for all individual panels to be removed by hand (alu panels) or by using a basic flat bladed tool (alu and steel panels).


PART 2: PRODUCT

________m2 Luxalon® 300L Wide Panel Carrier Ceiling consisting of:

2.1 PANELS:

Panels to be roll formed from 0.7 mm stove enamelled aluminium strip/0.6 mm thick stove enamelled galvanised steel strip, plain/ perforated with/without non-woven acoustic textile.

The 29 mm high upstands at the panel ends to give enhanced rigidity. The 300 mm wide panels to feature straight edges to form visually closed smooth joints.

Panels to be manufactured from pre-painted, stove enamelled aluminium, alloy EN-AW-3005 or equivalent (according to EN 1396 and ECCA)/from pre-painted, stove enamelled galvanized steel Z100 or equivalent metal coating (according to EN10169, part 3 and ECCA). Panels to have a length of______ mm. (manufacturer availability 1000-6000 mm and on request 250-1000 mm and > 6000 mm).


2.2 SUSPENSION:

Rows of 1.0 Fe/0.95 Alu roll formed carriers shall be installed at ________centre on centre (system maximum 2400 mm) by means of rigid suspensions at a distance of ______, centre of centre. Carriers will be joined by means of carrier splices. Carriers to include integrated locking clips to be used to lock the panels if required.


PART 3: ADDITIONAL SPECIFICATIONS

3.1 PERIMETER PROFILES

Wall L-profile, 29.2 x 19.4 mm made of 0.5 mm thick aluminium Wall L-profile, 45 x 18.5 mm made of 0.8 mm thick steel/aluminium Wall-W-profile, 45 x 21 x 21 x 18.5mm made of 0.8 thick steel/aluminium


3.2 PERFORATIONS

Manufacturer shall supply all 300L Carrier panels with the following perforation specifications:

Ø1.5 mm, ∆ 3 mm, open area 23 % Ø2.0 mm, ∆ 5 mm, open area 15%

Perforated panels to have a nominal plain border along the longitudinal panel direction to assure maximum product stability.


3.3 ACOUSTICS

Manufacturer shall supply acoustic non-woven tissue, thickness 0.2 mm and factory applied inside the panels. Alternatively the installer can place individual, wrapped mineral wool pads.


3.4 COATING

Architect will make a colour selection from the standard Hunter Douglas colour range for Luxalon® 300L Wide panels code no._______or a special colour will be made to match.

The coating will consist of a tough and durable 2-layer polyester finish in nominal thickness of 20 microns, applied in a continuous coil-coating process ensuring uniform coating and absolute adhesion.


3.5 INSTALLATION

All materials shall be installed in strict compliance with all local codes, ordinances and manufacturers recommendations including specific additional requirements as may be called for in the specifications or shown on the drawings.


3.6 SUBSTITUTIONS

Ceiling installers wishing to submit proposals on systems other than the Luxalon® 300L Wide Panel System shall, at least 20 days in advance of the bid date, submit to the architect complete descriptive information of the total system concept and performance data tests made as a system . In addition include a list of similar installations of the proposed substitution. If approval is made an addendum will be issued enumerating such approved system as herein set forth.