# LUXALON® EXTERIOR 84R CEILING SPECIFICATION

## PART 1: GENERAL

  - INTRODUCTION

Supply and fix Luxalon® Exterior 84R Ceiling system as manufactured by Hunter Douglas Architectural Products.

  - DESCRIPTION OF THE SYSTEM

The system will consist of round-edged linear panels fixed to a rigid suspension system, which allows for individual panels to be removed by hand. The suspension system consists of a non Luxalon® supporting structure. To prevent contact corrosion by applying dissimilar metals each fixing of the carriers to the sub-construction must be made through the Luxalon® washer set.

## PART 2: PRODUCT

_________ m² Luxalon® Exterior 84R Ceiling, consisting of:

2.1 PANELS

84R, size 84 x 15 mm manufactured from 0.6 mm aluminium.

Panels to be manufactured from prepainted, stove enamelled aluminium, corrosion resistant alloy EN-AW 3005 or equivalent (according to EN 1396 and ECCA). Panels have a length of _________ mm (manufacturer availability 1000-6000 mm and on request 250-1000 mm and > 6000 mm). Panels to be coupled in longitudinal direction by means of panel splices.

2.2 SUSPENSION

Rows of 0.95 mm aluminium rollformed carriers shall be installed at _________ centre on centre by means of a levelled suspension of sufficient strength and rigidity to provide resistance to wind pressure-/suction at a distance of _________, centre on centre. Carriers will be joined by means of carrier splices. Carriers provided with prongs to hold panels and infills with a total module of 100 mm.

## PART 3: ADDIOTIONAL SPECIFICATIONS

3.1 PERIMETER PROFILES

- Wall L-profile 45 x 18.5 mm made of 0.8 mm thick aluminium

- Wall W-profile 45 x 21 x 21 x 18.5 mm made of 0.8 mm thick aluminium

3.2 COATING

Architect will make a colour selection from the standard Hunter Douglas colour range for Luxalon® Exterior 84R panels code no. _________ or a special colour will be made to match.

The coating will consist of a tough and durable Luxacote® finish in a nominal thickness of approximately 20 microns, applied in a continuous coilcoating process ensuring colour stability. Luxacote® finish guarantees optimum adhesion and excellent resistance to weathering.

3.3 INSTALLATION

All materials shall be installed in strict compliance with all local codes, ordinances and manufacturers recommendations including specific additional requirements as may be called for in the specifications or shown on the drawings.