# LUXALON® V100-V200 SCREEN CEILING SYSTEM SPECIFICATION

## PART 1: GENERAL

  - INTRODUCTION

Supply and fix Luxalon( V100-V200 system as manufactured by Hunter Douglas Architectural Products.

  - DESCRIPTION OF THE SYSTEM

The system will consist of panels with profiled sides, clipped into an adjustable suspension system which allows for individual panels to be removed by hand.

## PART 2: PRODUCT

________m2  Luxalon( V100-V200 screen ceiling, consisting of:

  - PANELS

Panels, 101 mm or 200 mm high, with profiled sides (profile depth is 9 mm), to be manufactured from 0.6 mm thick prepainted, stove enamelled aluminium strip, alloy EN-AW-5050 or equivalent (according to EN 1396 and ECCA).

Panels have a length of ___________mm (manufacturer availability 1000-6000 mm and on request 250-1000 mm).

  - SUSPENSION

Rows of 0.95 mm Alu rollformed carriers, shall be installed at _____centre on centre by means of threaded rods or similar at a distance of _____,centre on centre. Carriers provided with cut-outs to hold panels in a standard module of 100 mm, 150 mm, or 200mm. Carriers will be joined by means of carrier splices.

Carriers provided with panel bracket assemblies consisting of 10 panel brackets and 9 spacers M = 100 mm, 150 mm or 200 mm. Panel stops to position the panel bracket assemblies (2 pcs per section of 10 panels).

## PART 3: ADDITIONAL SPECIFICATIONS

  - COATING

Architect will make a colour selection form the standard Hunter Douglas colour range for Luxalon® V100 and V200 panels code n. _____or a special colour will be made to match.

The coating will consist of a tough and durable polyester finish in nominal thickness of approximately 20 microns, applied in a continuous coil coating process ensuring uniform coating and absolute adhesion.

  - INSTALLATION

All materials shall be installed in strict compliance with all local codes, ordinances and manufacturers recommendations including specific additional requirements as may be called for in the specifications or shown on the drawings.