## PART 1. GENERAL

  - INTRODUCTION

Supply and fix type “Topline” Veneered Wood Wall/Ceiling panels as manufactured by Hunter Douglas Architectural.

  - DESCRIPTION OF THE SYSTEM

The system will consist of wood veneered tiles mounted into a  24 mm slotted tee bar system with the use of metal turn/screw clips.

## PART 2. PRODUCT

  - TOPLINE PANELS

________m2 type “Topline TLS/TTA” Veneered Wood Panels consisting of:

Linear panels of 128/256mm (module) foreseen with a tongue and groove connection. The panels have a 16mm thick FR treated MDF (B,S1-d0) core veneered with 0.6mm thick mis/slip/book matched veneer on the visible side. A 0.6mm compensating veneer and non woven acoustic fleece is adhered to the reverse of the tile.

  - SUSPENSION

Consists of pre-punched main tee sections installed in a grid by means of inserting cross tees which are designed to be used with the Topline panels.

## PART 3: ADDITIONAL SPECIFICATIONS

  - EDGE COVER PROFILES

- L-profile 29 x 19 mm made of 1.5 mm thick aluminium in white colour

  - PERFORATIONS

Manufacturer shall supply tiles with perforation pattern type TLS/TTA.

The TLS/TTA perforation consists of a 2/3/4mm groove on the view side, and slots/holes on the reverse side. The type of TLS perforation is TLS 5/3 – 6/2 – 13/3 – 14/2 – 28/4 – 29/3.

  - ACOUSTICS

Manufacturer shall/shall not supply acoustic non woven textile, thickness 0.2mm  glued on reverse tile side.

  - VENEER TYPES

Tiles shall be supplied with crown/quarter cut veneer ___________ mis/slip/book matched selected from the Hunter Douglas veneer selector or a special veneer.

Samples shall be supplied for approval prior to order.

The veneer is lacquered with a UV-polyacrylate varnish.

  - INSTALLATION

All materials shall be installed in strict compliance with all local codes, ordinances and manufacturers recommendations including specific additional requirements as may be called for in the specifications or shown on the drawings.

  - SUBSTITUTIONS

Ceiling installers wishing to submit proposals on systems other than the Hunter Douglas Topline panels shall, at least 10 days in advance of the bid date, submit to the architect complete descriptive information of the total system and performance data of tests made as a system. In addition include a list of similar installations of the proposed substitution. If approval is made an addendum will be issued enumerating such approved system as herein set forth.