| Product: | Hunter Douglas® Sun Louvre System 110HC |
| --- | --- |
| System: | Fixed system |
| Shape: | H-shaped curved panels |
| Panel section: | 121.2 x 94 mm, typical thickness 2.0 mm |
| Panel length: | max. 6000 mm |
| Alloy: | EN-AW 6060 T66 |
| Treatment: |  Mill finish  Anodised in 20 micron thickness: VB6/VOM1  Polyester powder coated 60 micron glosslevel 60% |
| Colour: | According RAL or NCS standard colour chart |
| Panel fixing: |  With nylon spacer block, module 142 mm, width 20 mm, shadow angle 75°  With nylon spacer block, module 162 mm, width 20 mm, shadow angle 70° |
| Spacer block: |  Colour white  Colour black  Colour silver |
| Panel module: |  142 mm module  162 mm module |
| Support system: |  Anodised aluminium extruded supporting arms for panels and spacer blocks  Wall brackets fixed to building |
| Installation: | Wall brackets fixed to the building, supporting arm slides over the wall brackets, panels and distance pc's slide in the supporting arms and finished with rectangular profile in front Option: Finished with bull-nose profile in front |